BETTOSEAL NP 100

2 Component Flexible Waterproofing Slurry

- BETTOSEAL NP 100 is a cement and polymer dispersion-based, two-component, fully flexible waterproofing material that prevents moisture, leakage and surface water on concrete surfaces, and can be applied negatively and positively.

- Fields of Application

• Indoor - outdoor, vertical and horizontal applications,

• On terraces (provided that it is protected)

• In soft water (PH = 3-7) storage pools used in the textile industry,

• In air conditioning pools, Olympic swimming pools and thermal pools,

• In water tanks,

• Wall and floor coverings of cold storages In all wet areas of the building such as WC, bathroom, kitchen

• As a part of the basic waterproofing system, in areas sensitive to movement, vibration and light settlements,

• Protecting concrete from carbonation, water and de-icing salts,

• In waterproofing in foundation curtain concrete

- Technical Data

| - BETTOSEAL NP 100 COMP A | - Cement, mineral fillers, special additives |
| --- | --- |
| - BETTOSEAL NP 100 COMP B | - Copolymer Acrylic dispersion |
| - Color | - Grey |
| - Adhesion Strength | - > 1.50 N/mm2 |
| - Water penetration | - 1 bar negative pressure , 1,5 bar positive pressure |
| - Cappilary water absorption | - Max 0,1 kg/m2 h0,5 |
| - Water vapour class | - Class 1 |
| - Substrate temp. | - +50C +300C |
| - Service temp. | - -200C +800C |
| - Pot life | - 45 min. |

- Application Method

- Preparation of Substrate

- The substrate must be sound, mainly even and fine-pored in the surface. It must be free of honeycombs, gaping cracks and ridges, dust, water repellents, form oil, paint or other bond-inhibiting residues. Fill voids and honeycombs with suitable repair mortar.

- The cemetitious substrate must be thoroughly prewet. It must be damp at the time of application, but must not be overwatered.

- Mixing of both components

- 25 kg A component mixed with 10 kg B component

- Mixed density 1,45 kg/lt

- Place 10 kg of Bettoseal NP 100comp.B in a clean mixing container and add 25 kg Bettoseal NP 100 Component A and mix to a lump free consistency. To ensure a lump-free mixing it is recommended to place only part of the required liquid component in the mixing container and mix with the powder component. The remaining liquid component will be added after the mixture is homogeneous enough.

- Consumption

- In three layers 4,2 kg/m2. (1,5 kg/m2 first layer, 1,3 kg/m2 second layer, 1,3 kg/m2third layer)